## Slide 1
Study of structural and magnetic properties of Nd substituted Sr2SnO4 orthostannate
by
SHAIL UPADHYAY
Associate Professor
DEPARTMENT OF PHYSICS
Indian Institute of Technology (BHU)
Varanasi, India

## Slide 2: Ceramic oxides crystallize in various structure such as ;
Rock salt – MgO, CaO, SrO etc
Wurtizite -- ZnS
Zinc blende -- BeO
Spinel -- ZnFe2O4 , CdFe2O4 , MgFe2O4
Corundum -- Al2O3
Rrutile -- GeO2, PbO2, MnO2
Cesium chloride -- CsCl
Fluorite -- ThO2, TeO2, VO2
Antifluorite -- Li2O3 , Na2O, K2O
Perovskite -- BaTiO3 , SrTiO3 , BaSnO3

## Slide 3: Pervoskites Structure
Discovered in the Ural mountains of Russia by Gustav Rose in 1839 and is named after Russian mineralogist L. A. Perovski
General chemical formula is ABX3, where 'A'
and 'B' are two cations of very different sizes,
and X is an anion (Cl, F, I and O).
Tolerance Factor (t) is in the
range of 0.75 – 1.0.

## Slide 4
Sr. No | Tolerance factor | Structure | Example
1. | >1 | Hexagonal | BaNiO3
2. | 0.9-1 | Cubic | SrTiO3 BaTiO3
3. | 0.71-0.90 | Orthorhombic Rhombohedral | GdFeO3 CaTiO3
4. | <0.71 | Triclinic,Tetragonal, etc. | FeTiO3

## Slide 5
Applications of perovskite oxides
Multilayer Capacitor - BaTiO3 , PMN, PMN
Piezoelelctric Transducer - Pb(Zr,Y)O3
P.T.C. Thermistor - BaTiO3
Elelctrooptical Modulator – (Pb,La)(Zr,Ti)O3
Switch – LiNbO3
Dielectric Resonator – BaZrO3
Thick Film Resistor – BaRuO3
Electrostrictive Actuator – Pb(Mg,Nb)O3
Superconductor - Ba(Pb,Bi)O3
Ferromagnet – (Ca,La)MnO3
Refractory Electrode – LaCoO3
Second Harmonic Generator – KNbO3
Magnetic Bubble Memory - GdFeO3
*Multi functional Sensor – BaTiO3 , BaSnO3, SrSnO3, NiSnO3

## Slide 6
Layered Pervoskite Oxide
This type of structure is first described in 1957 by S.N. Ruddlesden and P. Popper
General Chemical formula for layered pervoskite
oxide is An+1BnO3n+1 for n=1 A2BO4 It consist of ABO3 and a Layer of
AO are interconnected.

## Slide 7: Properties of Sr2SnO4
Its crystal structure is tetragonal and space group I4/mmm.
Tolerance factor t=0.97
Lattice parameters a=b= 0.4119 nm and c=1.2560 nm
Direct optical band gap 4.60 eV and indirect optical band gap 4.20 eV.

## Slide 8: Applications
Colossal magneto-resistance
Superconductivity
Spintronics
Ferroelectricity
Optical device .

## Slide 9: Motivation
Recently, rare earth (Eu3+ and Sm3+ and La3+) doped Sr2SnO4 materials have grabed attention due to their various optical properties, such as photoluminescence, mechanoluminescence, and up-conversion [26-34].Terbium doped Sr2SnO4 yellow pigments have shown high value of infrared reflectance, making it suitable for energy saving applications [35]. Nd3+ doped Sr2SnO4 has been explored for optical imaging.

## Slide 10
Weighing of compounds
(SrCO3, SnO2 and Nd2O3
Milling with acetone media in Ball-Miller for 8hr.
Drying
TGA/DSC
Calcination at 1000oC for 8hr.
XRD
Characterization: FTIR, Raman and Squid
Synthesis of Materials using Solid state reaction method

## Slide 11: TGA-DSC analysis of the Mixture of Sr1.98Nd0.02SnO4

## Slide 13
Composition (Sr2-xNdxSnO4) | Sample Code | Lattice Parameter(Ǻ) |  | Unit cell Volume (Ǻ3) | Theoretical density (gm/cm3) | Crystallite size (nm) | Reitveld refinement Parameters |  | 
 |  | a=b | c |  |  |  | Rp | Rwp | χ2
x=0 | S2NdS0 | 4.0527 | 12.5901 | 206.59 | 5.676 | 35.4 | 8.4 | 11.2 | 3.45
x=0.01 | S2NdS1 | 4.0532 | 12.5916 | 206.86 | 5.678 | 39.2 | 6.4 | 9.2 | 4.24
x=0.02 | S2NdS2 | 4.0523 | 12.5875 | 206.70 | 5.682 | 42.7 | 7.4 | 9.6 | 4.67
x=0.04 | S2NdS4 | 4.0535 | 12.5897 | 206.87 | 5.707 | 45.11 | 8.3 | 10.2 | 5.43
x=0.06 | S2NdS6 | 4.0529 | 12.5876 | 206.77 | 5.738 | 46.54 | 8.8 | 10.8 | 6.21
x=0.10 | S2NdS10 | 4.0530 | 12.5871 | 206.76 | 5.750 | 48.97 | 9.4 | 11.6 | 5.42
Table : Parameters obtained from Reitveld refinement of XRD profile.

## Slide 16
Magnetization vs Magnetic Field curve

## Slide 17
Magnetization vs. Magnetic Field for Sr2SnO4

## Slide 18
Magnetization vs. Magnetic Field for Sr1.98Eu0.02SnO4

## Slide 19
Magnetization vs. Magnetic Field for Sr1.90Nd0.10SnO4

## Slide 20: M-T Curve of Sr2SnO4

## Slide 21: M-T Curve of Sr1.98Nd0.02SnO4

## Slide 22: M-T Curve of Sr1.90Nd0.10SnO4

## Slide 23
Magnetization vs Temperature for all Nd-doped samples

## Slide 24
Study of Magnetization (M) vs. Magnetic Field (H) using Bound Magnetic Polaron(BMP) model

## Slide 25
Sample | Ms (emu/gm) (x 10-3) | Hc (Oe) | Mr (emu/gm) | N (/cm3) x 1020 | meff (x 10-24) | χ (emu/gm.Oe-1) x 10-7 | Mo= N.meff (x 10-3)
S2NdS0 | 4.15 | -40 | 1.64x10-4 | 8.56 | 7.26 | -2.593 | 6.21
S2NdS1 | 3.46 | -20 | 1.06x10-4 | 5.97 | 7.91 | -1.522 | 4.62
S2NdS2 | 25.65 | -18 | 2.06x10-5 | 0.06 | 35.18 | 2.362 | 0.211
S2NdS4 | 13.8 | -19 | 9.56x10-5 | 12.56 | 5.68 | 1.6985 | 7.13
S2NdS6 | 17.4 | -18 | 5.86x10-5 | 4.61 | 5.97 | 3.68 | 2.75
S2NdS10 | 35.2 | -23 | 8.07x10-5 | 4.34 | 6.55 | 8.084 | 2.84

## Slide 26
Thank you

## Slide 27
The thermal dependence of the susceptibility follows the modified curie-Weiss law given by;
χdc=χ0 + C/(T+θ); C=Nμeff2/3kB , N is the number of magnetic ions, μeff is the effective magnetic moment .
The dc susceptibility vs. temp curve have been fitted with the Curie –Weiss law , and after that subtracting the amount of χ0 then plotted 1/χ vs. T and shown in below;

## Slide 29
The K2NiF4 structure with general formula A2BO4 was first described by Balz and Plieth [1] for ternary oxide systems. These compounds are fabricated by depositing alternating layers of perovskite (ABO3) with sodium chloride (AO) type structure as interleaving layers [2]. These type of A2BO4 compounds belong to the Ruddlesdon-Popper series AO(ABO3). An extensive study of perovskite, related structures and their properties have been carried out by Goodenough and Longo [3]. The Ruddlesdon–Popper series with K2NiF4-type structure have enticed attention of researchers due to their interesting chemical and physical properties viz superconductivity [4], magnetoresistance [5,6], catalysis [7] and mixed ionic-electronic conductivity [8]. The structural and electrical properties of oxide material (with K2NiF4 - type structure) such NdBaInO4, La1−xSrxCoO4, Nd1.9Sr0.1CuO4, Nd1.8Sr0.2Ni0.6Cu0.4O4.01 have been studied extensively [9-13]. These mixed electronic-ionic conductors have received interest due to their high thermal stability, high oxygen diffusion coefficient, good electronic conductivity and strong electro-catalytic activity towards oxygen reduction reaction (ORR) [14] and capability to serve as cathode/electrolyte in solid oxide fuel cells (SOFCs) as well as solid oxide electrolysis cell (SOEC) devices [15,16]. Further an indispensable number of research studies have been conducted on Sr2MO4 compounds (with M= transition, post-transition or rare earth element like Sr2RuO4, Sr2RhO4, Sr2CuO4, Sr2VO4, Sr2SiO4, Sr2CeO4, etc.) doped with various lanthanide ions (from La3+ and Sm3+, Eu3+ to Yb3+) co-doped with alkaline ions (Li+, Na+, K+), although the main concern lies with its photoluminescence properties and applications (Phosphors, Solar cells etc.) [17-22]. The photoluminescence (PL) properties of various alkaline-earth orthostannates such as M2SnO4 (M= Ca, Sr and Ba) has been widely studied [23].
Strontium Orthostannates, Sr2SnO4 has an ordered tetragonal K2NiF4-type structure with space group I4/mmm; lattice parameters a and c as 4.052 and 12.580 Ǻ, respectively [24]. The direct and indirect band gaps of Sr2SnO4 are 4.67 and 4.20 eV, respectively [25]. Recently, rare earth (Eu3+ and Sm3+ and La3+) doped Sr2SnO4 materials have grabed attention due to their various optical properties, such as photoluminescence, mechanoluminescence, and up-conversion [26-34]. Terbium doped Sr2SnO4 yellow pigments have shown high value of infrared reflectance, making it suitable for energy saving applications [35].
The Sr2SnO4 system has been widely investigated for optical device application mainly concerned with its photoluminescence properties. Furthermore, it is observed that mainly the luminiscence properties of Eu doped only on Sr site, Sr2-xEuxSnO4 systems have been studied. In the structure of Sr2SnO4, the coordination number of Sr is 9 whereas for Sn it is equal to 6. The ionic radii of ions Sr2+ (in 9 co-ordinate state) and Sn4+ (6 co-ordinate state) are 1.31Ǻ and 0.69Ǻ, respectively. The ionic radii of dopant Eu3+ in respective states of 9 and 6 coordination number are 1.12 Ǻ and 0.95 Ǻ.

## Slide 30
Dietrich Balz and K. Plieth. "Die Structure des Kalium nickel fluorids, K2NiF4." Berichte der Bunsengesellschaft für physikalische Chemie 59, no. 6 (1955): 545-551.
S. N. Ruddlesden and P. Popper. "New compounds of the K2NiF4 type." Acta Crystallographica 10, no. 8 (1957): 538-539.
J. B. Goodenough and J. M. Longo. Crystallographic and magnetic properties of perovskite and perovskite-related compounds. Landolt-Bornstein 4 1970 126-314.
D. Hohlwein, A. Hoser, R. Sonntag, W. Prandl, W. Schäfer, R. Kiemel, S. Kemmler-Sack, and A. W. Hewat. Structural changes in superconducting La1.8Sr0.2CuO4 by alloying copper with cobalt. Physica B: Condensed Matter 156 (1989): 893-896.
M. Zaghrioui, F. Giovannelli, N. Poirot D. Brouri, and I. Laffez. Anomalies in magnetic susceptibility of nonstoichiometric Nd2NiO4+δ (δ= 0.049, 0.065, 0.077, 0.234). Journal of Solid State Chemistry 177 2004 3351-3358.
Takashi Matsuura, Junji Tabuchi, Junichiro Mizusaki, Shigeru Yamauchi, and Kazuo Fueki. Electrical properties of La2−xSrxCoO4—II: Models and analysis of the relationship between cobalt 3d electron state and structural, electrical and magnetic properties. Journal of Physics and Chemistry of Solids 49 1988 1409-1418.
Laitao Luo, Guangxin Shao, and Zhanhui Duan. Catalytic Oxidation Properties and Characterization of LaSrCo{0.9}B'{0.1}O4 (B'= Mn, Fe, Ni, Cu) Mixed Oxides. Turkish Journal of Chemistry 29, no. 6 (2006): 597-605.
E. Iguchi, H. Nakatsugawa, and K. Futakuchi. Polaronic conduction in La2− xSrxCoO4 (0.25≤ x≤ 1.10) below room temperature. Journal of Solid State Chemistry 139 1998 176-184.
Kotaro Fujii, Yuichi Esaki, Kazuki Omoto, Masatomo Yashima, Akinori Hoshikawa, Toru Ishigaki, and James R. Hester. New perovskite-related structure family of oxide-ion conducting materials NdBaInO4. Chemistry of Materials 26 2014 2488-2491.
Xiaoyan Yang, Shuaibo Liu, Fengqi Lu, Jungu Xu, and XiaojunKuang. Acceptor Doping and Oxygen Vacancy Migration in Layered Perovskite NdBaInO4-Based Mixed Conductors. The Journal of Physical Chemistry C 120 12 2016 6416-6426.
Cristina Tealdi, Chiara Ferrara, Piercarlo Mustarelli, and M. Saiful Islam. "Vacancy and interstitial oxide ion migration in heavily doped La2− x Sr x CoO4±δ." Journal of Materials Chemistry 22 2012 8969-8975.
Yasuo Kameda, Hiroshi Deguchi, Hirotoshi Furukawa, Yoshiyuki Kubota, Yasuyuki Yagi, Yoshihiro Imai, Noriko Yamazaki, Noriko Watari, Takuya Hirata, and Nobuyuki Matubayasi. "Hydration Structure of CO2-Absorbed 2-Aminoethanol Studied by Neutron Diffraction with the 14N/15N Isotopic Substitution Method." The Journal of Physical Chemistry B 118 2014 1403-1410.
Kotaro Fujii, Masahiro Shiraiwa, Yuichi Esaki, Masatomo Yashima, Su Jae Kim, and Seongsu Lee. Improved oxide-ion conductivity of NdBaInO4 by Sr doping. Journal of Materials Chemistry A 3 2015 11985-11990.
S. J. Skinner and J. A. Kilner. Oxygen diffusion and surface exchange in La2−xSr x NiO4+ δ. Solid State Ionics 13 2000 709-712.
A. Tarancón, Skinner, S.J., Chater, R.J., Hernandez-Ramirez, F. and Kilner, J.A., Layered perovskites as promising cathodes for intermediate temperature solid oxide fuel cells. Journal of Materials Chemistry, 17(30), 2007 pp.3175-3181.
H. Chaker, I. Raies, Chouket, A., Roisnel, T. and Hassen, R.B. Chemical and physical characterizations of the n= 1 Ruddlesden–Popper phases: Nd2− ySryNi1− xCoxO4±δ (y= 1 and 0.1≤ x≤ 0.9). Ionics, 2017 pp.1-12.
Frank. Lichtenberg, The story of Sr2RuO4. Progress in solid state chemistry 30 2002 103-131.
Tetsuo Shimura, Mitsuru Itoh, and Tetsurō Nakamura. Novel two-dimensional conductor Sr2RhO4. Journal of Solid State Chemistry 98 1992 198-200.
S. Smadici, J. C. T. Lee, A. Rusydi, G. Logvenov, I. Bozovic, and P. Abbamonte. "Distinct oxygen hole doping in different layers of Sr2CuO4−δ/La2CuO4 superlattices." Physical Review B 85 2012 094519.
Jérémie Teyssier, Enrico Giannini, Adrien Stucky, R. Černý, M. V. Eremin, and Dirk Van Der Marel. Jahn-Teller induced nematic orbital order in tetragonal Sr2VO4. Physical Review B 93 2016 125138.
Rahul Ghildiyal, Chia‐Hao Hsu, and Chung‐Hsin Lu. Aliovalent ion substitution and enhanced photoluminescence of Sr2SiO4: Tb3+/Z+ (Z= Li, Na, and K) phosphors. International Journal of Applied Ceramic Technology 8 2011 759-765.
R. Seema and K. Nanda Kumar. A new synthetic pathway of Sr2CeO4 phosphor and its characterization. Journal of Luminescence 131 2011 2181-2184.
Andrius Stanulis, Artūras Katelnikovas, David Enseling, Danuta Dutczak, Simas Šakirzanovas, Marlies Van Bael, An Hardy, Aivaras Kareiva, and Thomas Jüstel. Luminescence properties of Sm3+-doped alkaline earth ortho-stannates. Optical Materials 36 2014 1146-1152.
R. Weiss and R. Faivre. Préparation et structure de plombates et stannates alcalino-terreux du type A2BO4. Comptes Rendus Hebdomadaires Des Seances De L Academie Des Sciences 248 1959 106-108.
B. Prijamboedi, S. Umar, and F. Failamani. Electronic structure and optical properties of Sr2SnO4 studied with FP-LAPW method in density functional theory. In AIP Conference Proceedings vol. 1656 p. 030001. AIP Publishing, 2015.
Yu-Chung Chen, Yen- Hwei Chang, and Bin-Siang Tsai. Influence of processing conditions on synthesis and photoluminescence of Eu3+-activated strontium stannate phosphors. Journal of alloys and compounds 398 2005 256-260.
Xiaochun Zhou, Xiaojun Wang and Jiwu Wen. Optical study of Sr2SnO4: Eu3+ phosphor. Optik-International Journal for Light and Electron Optics 125 2014 3454-3456.
H. Zhao, Chai, X., Wang, X., Li, Y. and Yao, X., 2016. Mechanoluminescence in (Sr, Ca, Ba)2SnO4: Sm3+, La 3+ ceramics. Journal of Alloys and Compounds, 656, pp.94-97.
Takahiro Yamashita and Kazushige Ueda. Blue photoluminescence in Ti-doped alkaline-earth stannates. Journal of Solid State Chemistry 180 2007 1410-1413.
H. M. Yang, J. X. Shi, and M. L. Gong. A new luminescent material, Sr2SnO4: Eu 3+. Journal of alloys and compounds 415 2006 213-215.
Xuhui Xu, Yuhua Wang, Yu Gong, Wei Zeng, and Yanqin Li. Effect of oxygen vacancies on the red phosphorescence of Sr2SnO4: Sm 3+ phosphor. Optics express 18 2010 16989-16994.
K. Ueda, T. Yamashita, K. Nakayashiki, K. Goto, T. Maeda, K. Furui, K. Ozaki, Y. Nakachi, S. Nakamura, M. Fujisawa and T. Miyazaki,. Green, orange, and magenta luminescence in strontium stannates with perovskite-related structures. Japanese journal of applied physics, 45(9R) 2006 p.6981.
Sunao Kamimura, Hiroshi Yamada and Chao-Nan Xu. Strong reddish-orange light emission from stress-activated Srn+ 1SnnO3n+1: Sm3+ (n= 1, 2,∞) with perovskite-related structures. Applied Physics Letters 101 2012 091113.
M. Srinivas, B. Appa Rao, M. Vithal and P. Raghava Rao. "Luminescence properties of Tb3+ doped Sr2SnO4 green phosphor in UV/VUV regions." Luminescence 28 2013 597-601.
Athira KV Raj, P. Prabhakar Rao, S. Divya and T. R. Ajuthara. Terbium doped Sr2MO4 [M= Sn and Zr] yellow pigments with high infrared reflectance for energy saving applications. Powder Technology 311 2017 52-58.

## Slide 31: Properties of Neodymium (Nd)
Ionic radii in 9th coordination 1.35 Å
It forms very light grayish-blue hexagonal crystals
Neodymium(III) oxide is used to dope glass, including sunglasses, to make solid-state lasers.
neodymium-doped glass is dichroic; that is, it changes color depending on the lighting
Electron configuration [Xe] 4f4 6s2
Magnetic ordering :paramagnetic, antiferromagnetic below 20 K
Magnetic susceptibility : +5628.0·10−6 cm3/mol (287.7 K)